# MANUFACTURING CONCEPTS FOR VOLUME PRODUCTION

# OF LARGE COMPOSITE COMPONENTS

# Dr John Summerscales

Advanced Composites Manufacturing Centre

School of Manufacturing, Materials and Mechanical Engineering

University of Plymouth

Plymouth  PL4 8AA

United Kingdom

Traditionally fibre reinforced plastics have been manufactured using labour intensive methods, such as "bucket and brush" for boats and civil engineering structures, or "scissors and paste" for aero-space use.  The principal constraint on the wider application of polymer matrix composite materials in the construction industry is the need to develop systems to manufacture large numbers of parts to accurate tolerances with high quality and consistent appearance.

This paper considers the potential for efficient manufacture of composite components for the building industry, through a review of processes currently used or in prospect for the creation of large reinforced plastic structures.

ADVANCED POLYMER MATRIX COMPOSITES				FIBRE REINFORCED PLASTICS

MANUFACTURING CONCEPTS		FILAMENT WINDING		PULTRUSION

RESIN TRANSFER MOULDING		CENTIFUGAL CASTING	TAPE LAYING

## INTRODUCTION

# Traditionally fibre reinforced plastics are manufactured using labour intensive methods, such as "bucket and brush" for boats and civil engineering structures, or "scissors and paste" for aerospace use.  The principal constraint on the wider application of polymer matrix composite materials in the construction industry is the need to develop systems to manufacture large numbers of components to accurate tolerances with high quality and consistent appearance.

# This paper considers the potential for efficient manufacture of composite components for the building industry, through a review of processes currently used or in prospect for the creation of large reinforced plastic structures.  Finally the availability of courses on these techniques is addressed.

## MANUFACTURING CONCEPTS

### Pultrusion

# Pultrusion is a continuous process for manufacturing composites that have a continuous cross-sectional shape.  The process consists of pulling the fibre reinforcement through a resin impregnation bath and then through a heated shaping die where the resin is cured.

# Goldsworthy [1982] has described the adaptation of pultrusion for the construction of large diameter tanks on site.  The tank erection system is a pultrusion machine in a 12-metre trailer.  The unit is driven to the tank site and the total length of a specially designed profile (determined by the profile width, tank diameter and tank height) is pultruded into a storage cannister.  The trailer can then move to the next site.  The pultrusion has a groove on one edge and a tongue on the other.  The erection machine backfeeds from the cannister, meters bonding resin into the groove and hardener onto

the tongue, and interlocks each layer in a helical fashion to produce the tank.  The further potential for continuous production of submarine pipes and in-situ manufacture in space is noted.

# The use of pultrusion in the manufacture of skeletal structures has been extensively studied by Hollaway.  Most geometrical shapes can be produced by this technique, but the application was severely hindered by the inability to effectively join the pultrusions.  Two jointing systems [Green & Phillips, 1982 and Hollaway & Baker, 1984] have now made it possible to join pultruded sections at any angle allowing the fabrication of plane and space grid structures

Pultrusion technology has been used to produce a 16 000 sq.m. floor suspended below the A19 road Tees viaduct in Northern England [Head & Churchman, 1989, Wolfendale, 1988].  Five different pultrusions are assembled to produce 3-metre by 11-metre panels, which are further combined to produce a structural floor which is used both for maintenance access and as a protective cladding with a 30-40 year life in an industrial environment.  Twenty four kilometres of the main pultruded section were used.

# Exciting new projects, only possible with composites, have been proposed.  One such project would be an advanced composite suspension bridge across the Straits of Gibraltar [Meier, 1983, 1984 1987], although this scheme would consume the equivalent of several years production of carbon fibres.  The technology to produce the tension members is already established [Yeung & Parker, 1987].

# For applications where the transverse strength of a pultrusion would be too low, Shaw-Stewart [1988] has described a pullwinding technique.  One or more winding heads are mounted between the resin impregnation bath and the heated die of a pultrusion machine. Profiles can have thinner walls than conventional pultrusions.

### Sequential moulding

# Sequential moulding is a semi-continuous process for moulding continuous profiles from either thermoset or thermoplastic matrix materials.  Feedstock material is alternately pressed between heated dies in the platens of a closed down-stroking press, or translated along the die length by a distance shorter than the die length during the press open phase.  Because translation occurs with the die open, the forces required are much reduced.  It thus becomes possible to mould very thin profiles of large surface area which would be incapable of taking the tractive forces in pultrusion [Bowen, 1988].

### Filament winding

# Filament winding is a process for the manufacture of composite structures in which continuous fibre reinforcement is impregnated with resin then wound onto a rotating mandrel (removable former) in a predetermined pattern.  The shape is usually a surface of revolution.  When sufficient material has been wound the mandrel may be transferred to curing oven.  Filament winding is used to produce large diameter cylindrical pipes for water mains, and for effluent drainage. Filament wound segments have also been used to reline sewerage pipes.

# Covington and Baumgardner [1980] reported the development of prototype fibreglass helicopter rotor blades using filament winding techniques.  A Goldsworthy Orbital Pin Winding machine for high volume production of blades with longitudinal unidirectional reinforcement could lay approximetely 40 kg/hour of fibreglass using 16 strands of 60-end count prepreg roving.  The machine was 14 metre long, 4.5 metres wide and weighed 13 tonnes.  Addition of a second winding head could almost double production rates.  A McClean-Anderson tube winding machine could lay in excess of 27 kg/hour of a similar prepreg roving.

# McLarty [1981] analysed the feasibility of filament winding on a hull shaped mandrel in such a way as to cover the mandrel with fibres at a variety of angles to yield a structure conforming to the contours of the mandrel.  The feasibility was verified by winding a 1/48 scale hull.  It was concluded that 62 metre ship hulls could be produced.

# Chappelear et al [1983] conducted further study toward the filament winding of a 46-metre glass reinforced plastics ship hull, and developed a 1/5 scale mandrel for the proposed MSH mine sweeper-hunter for the United States Navy.

### Tape laying

# Tape-laying is similar to filament winding, except that the substrate is generally stationary.  The adjustment of fibre tension is thus more critical to avoid plies peeling from the substrate.

# Holt [1986] has described the development of tape-laying machines at Westland Helicopters for the production of composite main rotor blade spars.  For the Sea King blade project, the tape-laying head traversed an 11-metre flat bedway.  The head removed both the protective front film and the backing paper to lay down 10 plies of the prepreg material.  These plies were hand laid into the tool and consolidated with an inflating mandrel.

# To develop a second generation machine the fundamental problem was to automate the laying of material into a twisting and tapering tool cavity.  For the Lynx W30 series BERP blade an extensive programme was undertaken to develop appropriate material packaging technologies and brush laying techniques.  Consolidation of the irregular surfaced stack by brushes can accommodate tool shapes but required careful control of reinforcement tension and material guidance systems.

# The third stage of automation required the elimination of manual intervention in the process at material changeovers or reel replacement stages.  The result was a computer controlled CADAM system which is 16 metre long and will accept a range of mould tools.  Eight cassettes of material, each 'flagged' with faults by the prepreg supplier, are loaded into the machine.  A detector on the machine recognises the flags 11-metres ahead of the fault and can discard unsuitable material before beginning to lay a complete ply.

# Evans [1988] has described a two-stage tape-layer for the processing of 75 mm preimpregnated unidirectional carbon fibre tapes.  An off-line tape-processor inspects the tape and uses ultrasonic knives to prepare a reel of backing paper on which only good usable fault-free material is retained.  Cutting may be straight, angled of contoured.  The reel is logged into a computer for use by the second stage applicator.  The applicator does not carry cutting heads or ancillary equipment, and hence may be lightweight and very fast.  Tape is laid in one direction, with the substrate table rotated for oriented plies.  Lay-up speeds of up to 15 kg prepreg/hr are claimed

### Fibre arranging process

# The use of robots for composite manufacture offers considerable potential.  Automation of fibre cutting, textile handling, preform placement, bonding, painting and component machining are all amenable to automatic control.  Boyce [1989] has recently considered the use of robots in the winding of resin-impregnated fibres around pins to preform the reinforcement before compression moulding.

### Centrifugal casting

# Centrifugal casting is a production technique for fabricating cylindrical components, such as pipes.  The resin and fibres are rotated inside a hollow mandrel, which is rotated and heated to effect cure.

# Centrifugal casting is used to produce large diameter cylindrical pipes for water mains, and for the manufacture of telegraph poles, [Cheshire, 1988].

### Resin transfer moulding

# Resin Transfer Moulding (RTM) is a closed mould technique in which the mould is loaded with dry fibres before catalysed resin is injected under pressure or caused to flow into the mould by vacuum.  RTM has been used for some time in the production of motor car bodies [Adams & Roberts, 1985], boat hulls [Anon, 1986 a,b] and the Laser 28 deck [Pittman, 1985].

# Le Comte bV [Anon, 1986 c,d] produce a series of simple versatile reinforced plastic landing craft up to 22 metres long using vacuum-assisted injection moulding (VAIM) and has proposed that the 5 ton hulls of 34 metre surface effect ships will be produced using the VAIM technique.

### THE ADVANCED COMPOSITES MANUFACTURING CENTRE

# In November 1986, the United Kingdom Department of Education and Science offered start-up funding for new courses in Advanced Manufacturing Technology.  The University of Plymouth (then Plymouth Polytechnic) responded with a proposal for continuing professional education (CPE) to address the needs of the fibre composites manufacturing industry.  The Advanced Composites Manuafacturing Centre (ACMC) was set up in 1987 to deliver these CPE courses and to be a focus for research, development and consultancy.

# ACMC is the only establishment in Europe providing regular Short Courses for industry on manufacture of continuous-fibre reinforced plastic matrix composites.  The Centre also organises Workshop meetings where experts gather to discuss the underlying science of composite fabrication.  During the first 27 months there were 440 delegates from 192 companies, with 24% representation from overseas (EEC, Scandinavia, Austria, Switzerland, South Africa, Japan, Brazil, USA and Canada).

# For the future ACMC intends to run at least eight short courses and three workshops in each year.  Short course topics are repeated each year.  The workshop meetings address current 'hot' topics in composites manufacture. Recent meetings have addressed Thermoplastic Composites, Resin Transfer Moulding, Boatbuilding, Textiles and Preforms, Mould Tools, and Machining, Bonding and Repair.

# The provisional calendar to the end of 1991 includes both Short Courses (SC) and Industrial Workshops (W):

17-21 Sep 90	SC17	Introduction

10-12 Oct 90	SC18	Composites in motor racing

5-8 Nov 90	SC19	Filament winding

20-22 Nov 90	W13	Offshore composites

10-12 Dec 90	SC20	Cure monitoring

21-24 Jan 91	SC21	Advanced thermoplastic composites

11-15 Feb 91	SC22	Improved and automated manufacture

4-8 Mar 91	W14	Textiles and preforms

18-22 Mar 91	SC23	Practical composite tooling

22-26 Apr 91	SC24	Resin transfer moulding

13-17 May 91	SC25	Pultrusion

3-7 Jun 91	SC26	Foams and sandwich structures

17-21 Jun 91	W15	Sandwich structures

16-20 Sep 91	SC27	Introduction

7-11 Oct 91	SC28	Machining, bonding and repair

21-25 Oct 91	W16	Manufacture of FRP boats

11-15 Nov 91	SC29	Filament winding

9-13 Dec 91	SC30	Process monitoring and control

# The Centre has recently developed a Composites Engineering degree which was validated in June 1989.  The first students on this unique B.Eng.(Hons) Composites Engineering course will graduate in academic year 1990/91.  During the first two years the students will have gained a solid foundation in either Mechanical Engineering or Systems Engineering.  The third year will be spent in industrial training.  The final year concentrates on Composites Engineering with four 45-hour taught modules, a 60-hour practical module and a 160-hour research project.

### SUMMARY

# The manufacture of continuous fibre reinforced plastics as large structural components is practical using currently available techniques.  The paper has reviewed the most probable methods which may be used to produce such structures in large numbers with the consistency of appearance necessary for large projects.  The provision of education in these various techniques is also addressed

### REFERENCES

- Adams A.A. & Roberts J.H., 1985, "Vacuum impregnation", Proc.Conf.'Hands off GRP II', Coventry, 14 May 1985, Paper 5.

- Anon., 1986a, "Resin injection used in USA for moulding 21 foot cruiser hull", Reinforced Plastics, February 1986, 30(2), 48.

- Anon., 1986b, "Resin injection (RTM) powers off", International Reinforced Plastics Industry, Jan/Feb 1986, 5(3), 18.

- Anon., 1986c, "Injection moulding for large craft", Ship and Boat International, January/February 1986, 43-44.

- Anon., 1986d, "Solid skirts for smoother sailing", Ship and Boat International, January/February 1986, 25-26.

- Bowen D.H., Thorpe T., Hammond A. & Brabon S., 1988, "Sequential moulding- a process for continuous production of reinforced plastic profiles",  Proc.2nd.Int.Conf.Automated Composites, PRI/BCS/USAF, Leeuwenhorst NL, 26-28 September 1988, paper 27.

- Boyce G.S., 1989, "Development of a volume production technique for the manufacture of complex shaped components in continuous fibre composites", Proc.Mass Production Composites Symposium, Imperial College, London, 19-20 September 1989.

- Chappelear D.N, Aochi T. & Milligan R.J., 1983, "Filament winding of a ship hull", Lockheed report LMSC-D945 402, October 1983.  AD A134 577.

- Cheshire E.J., 1988, "The rise and fall of the Lampro telephone pole", Proc.16th Reinforced Plastics Congress, BPF, Blackpool, 7-10 November 1988, Paper 36, pp 163-166.

- Covington C.E. & Baumgardner, P.S., 1980, "Design and production of fibreglass helicopter rotor blades", In Lenoe, E.M., Oplinger D.W. & Burke J.J. (editors), "Fibrous Composites in Structural Design", Plenum, NY & London, 1980, pages 497-513.

- Evans G.J., 1988, "The processing of pre-impregnated composite materials",  Proc.2nd.Int.Conf.Automated Composites, PRI/BCS/USAF, Leeuwenhorst NL, 26-28 September 1988, paper 8.

- Goldsworthy W.B., 1982, "Continuous manufacturing processes", Chapter 17 in Lubin G. (editor), "Handbook of Composites", Van Nostrand Reinhold, 1982, pages 479-490.

- Green A.K. & Phillips L.N., 1982, "Crimp bonded end fittings for use in pultruded composite sections", Composites, July 1982, 13(3), 219-224.

- Head P.R. & Churchman A., 1989, "Design, specification and manufacture of pultruded composite floor", Proc.Mass Production Composites Symposium, Imperial College, 19-20 September 1989.

- Hollaway L. & Baker S., 1984, "The development of nodal joints suitable for double layer skeletal systems made from fibre/matrix composites", Proc.3rd.Int.Conf.Space Structures, Guildford, September 1984.

- Holt D., 1986, "Mechanised manufacture of composite main rotor blade spars", Proc.2nd.Int.Conf.Fibre Reinforced Composites, IMechE/PRI/IProdE/RAeS, Liverpool, April 1986, 125-131.

- McLarty J.L., 1981, "Feasibility of filament winding large ship hulls", McClean-Anderson report J2016, December 1981.  AD A125 771.

- Meier U., Muller R. & Puck A., 1983, "FRP-box beams under static and fatigue loading", Proc.Int.Conf.Testing, Evaluation and Quality Control of Composites, Guildford, 13-14 September 1983, pp 324-336.

- Meier U., 1984, "Multiplication of the critical span of suspension bridges through the use of high performance composites", Proc.14th.Reinforced Plastics Congress, BPF, Brighton, 5-7 November 1984, Paper 40, pages 185-187.

- Meier U., 1987, "Proposal for a carbon fibre reinforced composite bridge across the Strait of Gibraltar at its narrowest site",Proc.Institution of Mechanical Engineers, 1987, 201(B2), 73-78.

- Pittman K.L., 1985, "Breaking the old moulds", Sail, January 1985, 76-81.

- Shaw-Stewart D.E., 1988, "Pullwinding",  Proc.2nd.Int.Conf.Automated Composites, PRI/BCS/USAF, Leeuwenhorst NL, 26-28 September 1988, paper 15.

- Wolfendale R., 1988, "The A19 GRP enclosure - a highly visible GRP project", Proc.16th.Reinforced Plastics Congress, BPF, Blackpool, 7-10 November 1988, Paper 35, p 161.

- Yeung Y.C.T. & Parker B.E., 1987, "Composite tension members for structural applications", Proc.4th.Int Conf.Composite Structures, Paisley, 27-29 July 1987, volume 1, pages 309-320.